## Slide 1: Leather Industry
Prof. Dr. Abdullah Khan Durrani

## Slide 2: Leather
Leather is a durable and flexible material created via the tanning of putrescible animal raw hide and skin, primarily cattle hide. It can be produced through different manufacturing processes, ranging from cottage industry to heavy industry.

## Slide 3: Uses

## Slide 7
Skin
Hide
Leather
Raw Materials
(Goat, Buffallo, Cow etc)

## Slide 8: Composition of Skin 3 Layers

## Slide 9: Skin/Hide into leather
Vegetable Tanning
Chemical Tanning (Chrome Tanning)

## Slide 10
1-Vegetable-tanned leather is tanned using tannin (hence the name "tanning") and other ingredients found in vegetable matter, tree bark, and other such sources. It is supple and brown in color, with the exact shade depending on the mix of chemicals and the color of the skin. Vegetable-tanned leather is not stable in water; it tends to discolor, and if left to soak and then dry it will shrink and become less supple and harder. In hot water, it will shrink drastically and partly gelatinise, becoming rigid and eventually brittle. Boiled leather is an example of this where the leather has been hardened by being immersed in hot water, or in boiled wax or similar substances.

## Slide 11
2. Chrome-tanned leather, invented in 1858, is tanned using chromium sulfate and other salts of chromium. It is more supple and pliable than vegetable-tanned leather, and does not discolor or lose shape as drastically in water as vegetable-tanned. Also known as wet-blue for its color derived from the chromium.

## Slide 12
3. Aldehyde-tanned leather is tanned using glutaraldehyde or oxazolidine compounds. This is the leather that most tanners refer to as wet-white leather due to its pale cream or white color. It is the main type of leather used in chrome-free leather often seen in infant's shoes and in automobiles that prefer a chrome-free leather. Formaldehyde tanning (being phased out due to its danger to workers and the sensitivity of many people to formaldehyde) is another method of aldehyde tanning.

## Slide 13
4. Synthetic-tanned leather is tanned using aromatic polymers such as the Novolac or Neradol types. This leather is white in color and was invented when vegetable tannins were in short supply, i.e. during the Second World War. Melamine and other amino-functional resins fall into this category

## Slide 14
5. Alum-tanned leather is tanned using aluminum salts mixed with a variety of binders and protein sources, such as flour, egg yolk, etc. Purists argue that alum-tanned leather is technically "tawed" and not tanned, as the resulting material will rot in water.

## Slide 15
6. Rawhide is made by scraping the skin thin, soaking it in lime, and then stretching it while it dries. Like alum-tanning, rawhide is not technically "leather", but is usually lumped in with the other forms. Rawhide is stiffer and more brittle than other forms of leather

## Slide 16: STAGES OF LEATHER FORMATION
Warehousing and sorting In the raw material area the skins are preserved in salt, stored in controlled cool rooms and before processing, presorted for quality and weight.
Soaking The skin is soaked to remove dirt and salt.
De-Fleshing During this process tissue, flesh and fat remnants are removed by a roller mounted knife.

## Slide 17
Liming By adding lime and sulphur compound the hair is removed from the skin.
Bating, pickling, tanning During bating and pickling the skins are treated with acid and salt in preparation for tanning. During tanning the skin fibres absorb the tanning agents. That's when the skin becomes leather.
Samming During this process water is removed.

## Slide 18
Splitting In order to achieve an even specified thickness the leather is reduced in substance. The resulting split-leather can than be processed further as suede.
Skiving The grain leather is brought to an even thickness. Irregularities are removed from the reverse side and the leather is separated into color-batches.

## Slide 19
Sorting The leather is sorted into various quality grades.
Neutralizing, filling out, dyeing and greasing The acid resulting from the tanning process is neutralized. Then the dyeing takes place, where appropriate with anilin-dye-stuffs. The greasing procedure will finally achieve the correct softness.
Drying Two methods are used to dry leather. The vacuum process during which moisture is removed by suction and the hanging process, when leather is hung and taken through ovens.

## Slide 20
Staking Following drying the leather is mechanically staked in order to soften it. Further processes take place in preparation for finishing.
Finishing Here the leather is given its final surface treatment and look. Through processes of base coat, coloring, embossing, ironing the leather becomes, depending on the demands of fashion, matt or shiny, two-tone or uni-coloured, smooth or grained. The art of finishing lies in working in wafer-thin layers without disturbing the natural look of the leather and its characteristics such as suppleness and breath ability.

## Slide 21
The conventional chrome tanning process employs basic chromium sulphate (BCS). Chromium has a tendency to precipitate at pH>4.0.

## Slide 22
Chromium III salts are used extensively in the tanning process. Approximately 90% of the leather manufactured is tanned using chromium III. This is because chromium is the most efficient and versatile tanning agent available and it is relatively cheap. It has been used in the leather industry for almost 100 years and when it was introduced as an alternative to vegetable tanning extracts from oak bark and similar sources

## Slide 23: Other Tannins
(a) acrylic syntans
(b) phenol, naphthol or related materials
(c)urea/formaldehyde resins and
(d)protein hydrolysates

## Slide 24
Conventional chrome tanning in leather processing discharges significant amounts of chromium,total dissolved solids and chlorides.Hence, tanners are looking for new product-process innovations towards low-waste and high exhaust chrome tanning. A polymeric syntan, which can enable chrome tanning using commercial basic chromium sulphate, has been developed